## Slide 1
Quality impact
Ceramic Stones Porcelain pollution
in Cullet
Hans Hilkes
Senior Quality Manager Glass Raw Materials - AGP
January 2026

## Slide 2
  Introduction
  Appearance
  Container Glass Plant
  Possible consequences of what slips through

## Slide 3
Cullet (or “recycled glass”) is the main raw material used in the production of container glass.
It is also the most polluted.
Introduction

## Slide 4
An example of contamination is the presence of stones, ceramics or porcelain.
Incoming glass materials at Glass recycling companies contain this to a greater or lesser extent as contamination next to the glass.
Possible causes,
Consumers who dispose of these materials incorrectly
Pollution of industrial glass streams like,
  Filler companies
  Horeca establishments
Introduction

## Slide 5
Glass recycling companies have advanced equipment to remove these and other contaminants.
Introduction

## Slide 6
To check if the Furnace Ready Cullet, delivered by the Glass recycling companies, is according specification requirements, Glass producers perform quality checks on incoming deliveries.
Introduction

## Slide 7
Cullet that isn’t according specification is rejected and returned to supplier
Examples shown are findings out of a 50 kg sample taken from an incoming delivery
Introduction

## Slide 8
  Introduction
  Appearance
  Container Glass Plant
  Possible consequences of what slips through

## Slide 9
C.S.P. (Ceramic, Stones, Porcelain)
Pieces of Ceramic, Stones, Porcelain found in deliveries of Furnace Ready Cullet

## Slide 10
C.S.P. (Ceramic, Stones, Porcelain)
Ceramic, Stones, Porcelain inclusions found in produced containers

## Slide 11
C.S.P. (Ceramic, Stones, Porcelain)
Ceramic, Stones, Porcelain inclusions found in produced containers under microscope

## Slide 12
  Introduction
  Appearance
  Container Glass Plant
  Possible consequences of what slips through

## Slide 13
Container Glass Plant
Process Overview
Because Recycling Cullet always has a certain level of pollution present, also in Container Glass Plants a lot of effort is put in sorting out products with defects (Inclusions, Cracks, etc)

## Slide 14
Container Glass Plant
Equipment in use: Camera Inspection Equipment
Removal of Products with inclusions, blisters and other visual defects

## Slide 15
Container Glass Plant
Equipment in use: Camera Inspection Equipment
Removal of Products with inclusions, blisters and other visual defects

## Slide 16
Container Glass Plant
Equipment in use: Camera Inspection Equipment
Removed Products with inclusions

## Slide 17
C.S.P. (Ceramic, Stones, Porcelain)
Big pieces of (glass) ceramic can cause blockage in IS machines, and start a fire
C.S.P. (Ceramic, Stones, Porcelain)

## Slide 18
  Introduction
  Appearance
  Container Glass Plant
  Possible consequences of what slips through

## Slide 19
Filler plants (at customers)
Breakage during filling process
What if these products reach end-consumers

## Slide 20
Filler plants (at customers)
Breakage after filling process, during transport
Red circle is point of origin of breakage, fortunately, did not reach the end-consumer

## Slide 21
Filler plants (at customers)
Not found at Glass plant / Filler
Product returned by end-consumer, caused injury to end-consumer when removing the closure

## Slide 22: Thanks for your attention